# SPECIFICATION

Quality							: Sparta

Product definition		:	tufted loop pile

Gauge	ISO 2424	:	1/10”

No. of tufts 	ISO 1763	:	173.360 /m2  (- 7.5%.   + 10%)

Pile fibre	ISO 2424	:	100%  PA SDN

Pile weight	ISO 8543	:  510 gr/m2 (± 5% )

Pile height	ISO 1765	:	3.5 mm (± 5%)

Primary backing	ISO 2424	:	PA/PES non-woven - Colback

Tile backing	ISO 2424	:	Polyflex

Total thickness	ISO 1765	:	5.2 mm (± 5%)

Total weight	ISO 8543	:	3800 gr/m2  (± 7,5% )

Tile size	EN 986	:	50 x 50 cm  (± 0.2 %)

Tiles per box		:	20

# PERFORMANCE

Use classification	EN 1307	 :	33

Castor chair test	EN 985	:	A, continuous use

Thermal isolation	ISO 8302	:	Ca. 0,07 m2 K/W

Luxery/Comfort			EN 1307		:  LC1

Sound Insulation	 		ISO 10140		: 24 dB

# ELECTROSTATIC PROPERTIES

Walk on test	ISO 6356	:	-0.1 kV

Horizontal electrical resistance	ISO CD 10965	:	3x108 

Vertical electrical resistance	ISO CD 10965	:	4x1010 

Static loading		:	anti-static

# FLAME PROPERTIES

Reaction to fire 	EN 13501-1	:	Bfl – s1

# COLOUR FASTNESS PROPERTIES

Light	ISO 105 B02	:	> 5

Rubbing, dry	ISO 105 X12	:	5.0

Rubbing, wet	ISO 105 X12	:	5.0

Shampoo	BS 1006	:	5.0

Water	ISO 105 E01	:	4.5

Water stains	TNO W 6024	:	5.0

# GENERAL

# Recommended maintenance:	Best results are obtained when cleaned with a dry shampoo method.

Pile direction:	Directional arrows are printed on the back of each tile.

Best results are obtained when laid checkerboard.

Laying instructions:	Tiles require no underlay, nailing, gluing or sewing and may be laid loose on a flat,

dry, non-slippery floor. When tiles are laid on parquet, vinyl or in open areas larger

than 30 m2 it is advisable to use double sided adhesive tape on every 8th row or a

tackifier.

COLOURS

| Col. 2778 |  |  | Col. 2777 | Col. 2772 |
| --- | --- | --- | --- | --- |
| Col. 2783 | Col. 2784 |  | Col. 2776 | Col. 2793 |
| Col. 27278 |  |  | Polyflex Backing | Felt Backing |

24.2.2023